## Slide 1: Aspects of Negative Ions in Microwave PECVD Plasmas for Diamond Thin Film Deposition
Michael P. Bradley
Professor, Physics & Engineering Physics & Dean, College of Engineering
University of Saskatchewan

## Slide 2: Diamonds!
Koh-i-noor
(Persian: light of the mountain)
Gemstone diamonds
Diamonds have fascinated humanity since ancient times.
In addition to their great natural beauty as gemstones, diamonds
were the hardest known natural material.

## Slide 3: Diamond to the physicist
Diamond to the physicist is a little more prosaic: it is carbon bonded in a tetrahedral configuration
The group-IV crystalline semiconductors silicon and germanium have this same lattice structure
 usually just called the diamond lattice

## Slide 4: Defects in Diamonds
Impurities (Dopants) give rise to coloured Diamonds, e.g.
Boron Blue
Nitrogen Yellow
https://www.capetowndiamondmuseum.org/blog/2019/05/5666/

## Slide 5: Diamond Growth
Naturally occurring diamonds are formed
mantle of the Earth, under conditions of
high temperature and pressure
In the laboratory, diamond films can be
grown using microwave plasma chemical
vapour deposition (MPCVD) using a
feedstock of methane gas with excess H2
Figure credit: geology.com

## Slide 6: Plasmas & Connection to Catalysis
In the laboratory, diamond films can be
grown using microwave plasma chemical
vapour deposition (MPCVD) using a
feedstock of methane gas with excess H2
Analogy to catalysis- energetic plasma electrons
enable reactions
Figure credit: geology.com

## Slide 7: Plasma Parameters
There are two basic plasma parameters:
Plasma density:
&
Plasma Temperature:
These parameters determine the plasma behaviour- they cover an extremely wide dynamic range

## Slide 8: Plasma Density & Temperature: a Very Wide Dynamic Range
Figure credit: LPP, Ecole Polytechnique, Palaiseau, France
Logarithmic scale. 1 eV ⟷ 11,608 K
1 eV
0.1 eV
10 eV
100 eV
1 keV
10 keV
100 keV
Plasma
Temperature
Scale:
1eV  11000 K

## Slide 9: Cold Plasmas- Not in Equilibrium
A plasma in equilibrium would have a common temperature T for all species (e.g. electrons and ions)
In practice, many laboratory cold plasmas for materials processing are non-equilibrium plasmas, with

## Slide 10: Cold Plasmas- Connection to Catalysis
Tgas ~ 350 K
Ti ~ 600 K
kBTe/e ~ 2-5 eV  Te ~ 20000 – 50000 K (!)
Analogy to catalysis- energetic plasma electrons
enable reactions

## Slide 11: MPECVD System Schematic

## Slide 12: Microwave Plasma-Enhanced CVD for diamond film growth
Microwave Plasma
Chamber
Frequency 2.45 GHz
Power: 500 - 800 Watt
Pressure: 23 - 100 Torr
Substrate Temperatures >500 C
Feed gas ratio ~ 99% H2/1% CH4
(excess hydrogen)
Film growth rate:
~ 0.1 – 1 𝜇m/hour

## Slide 13: Applications
Hard Coatings
Semiconductor Chip Applications
  Thermal conductivity of diamond ~ 2400 W/m.K (!)
  ~6x copper
N-doped Diamond Films: Diamond NV- Centres

## Slide 14: Growth of in-situ N-doped diamond films
Grown on p-doped (111) silicon
MPECVD Conditions:
30 Torr
800 Watt
Feed gas flow rates:
CH4 1 sccm
H2 100 sccm
During doping:
N2 10 sccm

## Slide 15: Growth of in-situ N-doped diamond films
Grown on p-doped (111) silicon
MPECVD Conditions:
30 Torr
800 Watt
Feed gas flow rates:
CH4 1 sccm
H2 100 sccm
During doping:
N2 10 sccm

## Slide 16: Signatures of Diamond: Raman line at 1332 cm-1
D.S. Knight and W.B. White, J. Mater. Res., Vol. 4, No. 2, Mar/Apr 1989

## Slide 17: Signatures of Diamond: Raman line at 1332 cm-1
IEEE TRANSACTIONS ON PLASMA SCIENCE, VOL. 53, NO. 10, OCTOBER 2025

## Slide 18: Signatures of Diamond: Raman line at 1332 cm-1
IEEE TRANSACTIONS ON PLASMA SCIENCE, VOL. 53, NO. 10, OCTOBER 2025

## Slide 19: XRD

## Slide 20: Photoluminescence Results

## Slide 21: NV- Photoluminescence (PL)

## Slide 22: PL Intensity and Film Structure
Less tightly packed films higher PL intensity

## Slide 23: Negative Ions in Processing Plasmas
Negative ions can form in materials processing plasmas:
Kono et al. measured negative ions in SF6, NF3, CF4, and C4F8 gases diluted with Ar
Used a laser photodetachment method combined with millimeter-wave resonance
At a molecular-gas mixing ratio as low as 5–10% and ne~1011 the negative ion density was comparable to or higher than the electron density.
Kono et al., Thin Solid Films 407 (2002) 198–203.

## Slide 24: Negative Ions in Processing Plasmas: Methane Feedstock
Hoshino et al. Negative ion formation in CH4 for electron energies from 6-11 eV
Resonant dissociative electron attachment ~ 10.3 eV
M. Hoshino et al. / International Journal of Mass Spectrometry 306 (2011) 51– 56

## Slide 25: Langmuir Probes for Negative Ion Measurements
Expecting that negative ions may be present in our hydrogen-methane diamond deposition plasmas, how to measure their density ?
Langmuir probe analysis ?
Ordinary Langmuir probe analysis: measures n+, ne, and Te
Negative ion Langmuir probe analysis attempts to measure an additional parameter n-: the negative ion density [1],[2]
Goal: measure the electronegativity parameter
[1] C. Poggi, et. al. “Measure of negative ion density in a large negative ion source using Langmuir probes”. 8th Symposium on Negative Ion Beams and Sources, JINST, 2022.
[2] J. Bredin, P. Chabert and A. Aanesland, “Langmuir probe analysis in electronegative plasmas”, Phys. of Plasmas 21l (2014) 123502.

## Slide 26: Langmuir Probe Equations [1], [2]
[1] C. Poggi, et. al. “Measure of negative ion density in a large negative ion source using Langmuir probes”. 8th Symposium on Negative Ion Beams and Sources, JINST, 2022.
[2] J. Bredin, P. Chabert and A. Aanesland, “Langmuir probe analysis in electronegative plasmas”, Phys. of Plasmas 21l (2014) 123502.
where:
For

## Slide 27: Langmuir Probe Equations
For
[1] C. Poggi, et. al. “Measure of negative ion density in a large negative ion source using Langmuir probes”. 8th Symposium on Negative Ion Beams and Sources, JINST, 2022.
[2] J. Bredin, P. Chabert and A. Aanesland, “Langmuir probe analysis in electronegative plasmas”, Phys. of Plasmas 21l (2014) 123502.

## Slide 28: Langmuir Probe Theoretical Curves (a=0 and a=3)

## Slide 29: Representative Data
800 W microwave discharge
Pure hydrogen (100 sccm)
P=30 Torr
Cylindrical Langmuir Probe
Aprobe= 25.3×10−6 m2

## Slide 30: Te
vs Voltage for Hydrogen at 800 W
Te = 3.4 eV

## Slide 31: Analysis
Using BRL analysis [1],[2]
with Te=3.4 eV and g=1.9
gives
If a=0 
 electron saturation current
is then predicted to be 21 mA
But….observed electron sat’n~ 6-7 mA
[1] M Tuszewski and J A Tobin 1996 Plasma Sources Sci. Technol. 5 640
[2] Laframboise J G 1966 University of Toronto Institute for Aerospace Studies Report 100

## Slide 32: Analysis II
Using electron sat’n current = 7 ma
Predicts
And hence a~3
 Non-trivial negative ion density ?

## Slide 33: Conclusions
Diamond films can be grown effectively on silicon substrates using MPECVD
This has many applications: hard coatings, thermal interface layer for advanced chip cooling, and NV- centre work
H2:CH4 plasmas are used for diamond film growth
Both hydrogen and methane plasma can contain negative ions
Therefore study of negative ion densities in MPECVD Chambers is relevant
Preliminary results suggest a~ 3 for common processing conditions

## Slide 34: Acknowledgements
Portia Switzer (see poster)
William Davis MSc thesis & current PhD work
Hammed Ejalonibu PhD thesis
SSSC for materials characterization
The diamond growth work was financially supported by the NSERC
Discovery Grants program as well as a Canadian Space Agency (CSA)
FAST grant for development of a compact spaceborne MRI

## Slide 35: Funders: NSERC, DND, CSA
NSERC Discovery Grants Program
NSERC/DND Defence Supplement
Canada-UK Joint-Quantum Technologies grant program (w/ M Squared Lasers (Glasgow), and Prof. Mark Fromhold of the University of Nottingham)
CSA FAST Grant with Prof. G. Sarty