## Slide 1
Ion Source Development
for AMS at WHOI
NIBS ’26
Sep 20 – 25, 2026
Nelson, British Columbia, Canada
Mark L. Roberts1 and Joshua D. Hlavenka1,2
1Woods Hole Oceanographic Institution
1,2Argonne National Laboratory

## Slide 2: What is AMS?
Accelerator mass spectrometry (AMS) is a method to count atoms of rare, long-lived radioactive isotopes (like 14C) by accelerating ions to high kinetic energies using an accelerator and separating isotopes by mass.
Schematic from ‘The Methodology and
Physics of AMS’, L. Keith Fifield

## Slide 3: One of two AMS systems at WHOI
CFAMS System

## Slide 4: Why a negative ion source? Why electrostatic tandem acceleration?
AMS uses a negative ion source to eliminate background interference from isobars.
An accelerator because molecular breakup in the high voltage terminal stripper eliminates molecular ions.
The best example of this is that 14N does not form a stable negative ion. If 14N made a negative ion, radiocarbon dating using AMS would not be possible.
For example, in 14C AMS, the terminal stripper destroys interfering 12CH2 and 13CH molecules.

## Slide 5: Principle of the Negative Ion Cesium Sputtering Source
Sample
Holder
Cs+ Ion
Trajectory
Cs Diffuser
Immersion
Lens
Negative Ions
Hot Tantalum
Ionizer
Extraction
Electrode
Heater
Cs From
Oven
-5 kV
-4.6 kV
O V
+ 20 kV
From ‘The Methodology and
Physics of AMS’, L. Keith Fifield

## Slide 6: Important Metrics for a Negative Ion Source
Ion Current
At 100 mA of 12C-, the 14C count rate from a modern sample is ~ 300 cps. Hence, to get to a total of 250,000 counts (0.2%) takes ~ 14 minutes
Efficiency
A 30 mg, 11,500 year old sample has ~ 370,000 14C atoms.
With a 10% source efficiency and 50% stripping efficency, we can only detect a maximum of ~ 18,000 14C atoms (0.7%).
Beam Emittance
Need a reasonably small beam emittance. Too large a beam emittance and isotope fraction becomes a problem.
The accelerator stripping canal diameter is typically the limiting factor.

## Slide 7: Ion Source Modeling
Numerical Electrodynamics Laboratory (NEDLab). A 2.5-dimensional (cylindrical or Cartesian) particle and field simulation software.
Important considerations:
  Child’s Law modeling (Cs+ from ionizer)
  Ion emission with thermal energy distribution and randomized angles
  Space charge

## Slide 8: Ion Source Modeling
Cs+
C-
Old electrode geometry
New electrode geometry
Model predicted 2X Current. In practice, currents increased from ~ 200 mA to ~370 mA.
From Brown, Roberts, and Southon
NIM B 172 (2000) 344-349

## Slide 9: Ionization potentials of Cs compared to the electron affinities of C and other elements,

## Slide 10: Different Cathode Material
Zinc Insert
Aluminum
Cathode
Graphite
Cross-section of NOSAMS cathode with zinc insert.
From http://www.periodictable.com

## Slide 11: Different Cathode Material
Chart: Time (min)
| 3 | 6 | 9 | 12 | 15 | 18 | 21 | 24 | 27 | 30 | 33 | 36 | 39 | 42 | 45 | 48 | 51 | 54 | 57 | 60 | 63 | 66 | 69 | 72 | 75 | 78 | 81 | 84 | 87 | 90 | 93 | 96 | 99 | 102 | 105 | 108 | 111 | 114 | 117 | 120 | 123 | 126 | 129 | 132 | 135
Zinc | 92.7451 | 101.7254 | 101.8238 | 103.8209 | 104.1549 | 103.9325 | 103.7952 | 103.7999 | 104.2725 | 102.9163 | 100.5085 | 99.9199 | 99.5784 | 99.0918 | 98.4392 | 97.2105 | 96.3733 | 96.0927 | 95.4768 | 95.0069 | 93.6607 | 94.6916 | 93.8707 | 94.6645 | 93.3554 | 91.6438 | 91.4603 | 90.5612 | 88.6178 | 89.1768 | 86.8405 | 87.7606 | 85.6356 | 81.4669 | 81.1678 | 78.838 | 75.5323 | 73.3052 | 69.776 | 67.6766 | 65.1452 | 61.6663 | 56.3007 | 49.7354 | 39.6003
Titanium | 17.2355 | 80.9992 | 85.5201 | 83.1221 | 81.9053 | 81.4294 | 84.347 | 84.4005 | 83.6331 | 81.5137 | 80.34 | 80.6209 | 79.5017 | 79.1327 | 78.2949 | 77.4243 | 77.1465 | 77.3357 | 76.2408 | 76.616 | 75.0698 | 74.1986 | 73.1549 | 73.8015 | 72.9962 | 72.2063 | 71.3427 | 71.8354 | 70.2157 | 70.2242 | 69.646 | 69.2758 | 68.7659 | 67.1182 | 66.1068 | 64.8889 | 64.3953 | 65.0546 | 64.0343 | 64.0601 | 63.2942 | 62.9667 | 62.4656 | 61.8683 | 61.6588
Aluminum | 74.3166 | 78.0245 | 72.5531 | 69.1519 | 67.1558 | 67.2425 | 63.6499 | 62.4827 | 66.0287 | 66.2775 | 62.6146 | 62.7088 | 59.683 | 57.6837 | 55.908 | 54.7641 | 55.0999 | 55.411 | 52.7297 | 52.2446 | 49.1887 | 50.0788 | 47.2599 | 45.3191 | 42.1268 | 41.2835 | 40.4213 | 39.7571 | 37.855 | 35.016 | 36.0671 | 38.4979 | 35.1657 | 35.703 | 33.5964 | 35.5751 | 39.2065 | 43.6056 | 37.5014 | 29.0937 | 26.3532 | 24.7558 | 22.4519 | 26.1707 | 23.489
Iron | 70.0843 | 73.4192 | 73.1134 | 70.969 | 69.3649 | 62.1963 | 60.9217 | 62.6358 | 63.2003 | 63.1545 | 63.9833 | 63.1199 | 64.0919 | 63.911 | 63.7147 | 63.4827 | 63.6797 | 64.6456 | 64.791 | 66.2434 | 64.4578 | 64.2235 | 63.585 | 63.904 | 63.1293 | 61.8041 | 61.122 | 61.2647 | 59.5477 | 58.9201 | 57.6547 | 57.2912 | 57.1005 | 55.095 | 55.308 | 53.6721 | 53.0954 | 52.9251 | 51.6613 | 52.4912 | 51.7309 | 50.2082 | 49.2086 | 49.6217 | 48.2251
Copper | 48.1292 | 54.6673 | 53.8528 | 52.2418 | 48.3647 | 45.7856 | 45.4798 | 42.3461 | 40.6995 | 39.0523 | 37.649 | 35.3599 | 34.3672 | 31.9409 | 29.9928 | 28.7999 | 27.8488 | 26.316 | 26.7334 | 25.7622 | 25.5381 | 23.9415 | 22.8591 | 22.5496 | 21.2266 | 20.6333 | 19.7689 | 18.0849 | 16.9906 | 15.356 | 14.7083 | 14.1945 | 14.6995 | 13.1398 | 13.5924 | 11.6329 | 10.4111 | 10.844 | 9.6541 | 10.2312 | 9.3887 | 9.2074 | 8.3799 | 8.6547 | 8.4262
Molybdenum | 68.4703 | 74.2087 | 70.7963 | 63.6563 | 58.2235 | 58.8762 | 57.0566 | 54.5338 | 52.2906 | 50.9029 | 46.6418 | 39.22 | 39.1736 | 40.5829 | 39.7991 | 39.6365 | 36.6913 | 33.8978 | 33.8458 | 33.6582 | 34.3302 | 33.6775 | 32.3988 | 31.5228 | 30.1126 | 28.645 | 28.2065 | 29.0473 | 28.5477 | 27.8175 | 25.0444 | 25.673 | 28.5615 | 27.7953 | 28.5296 | 28.6296 | 27.0796 | 27.9239 | 27.3045 | 26.6396 | 28.2337 | 28.045 | 27.2299 | 26.6439
Nickel | 22.7403 | 26.936 | 27.2608 | 28.2409 | 27.5242 | 29.1443 | 29.5848 | 28.5367 | 27.1027 | 27.1361 | 26.7785 | 25.1115 | 25.7365 | 24.958 | 25.044 | 24.6745 | 23.2851 | 23.2397 | 23.8327 | 23.3789 | 22.4043 | 22.1553 | 22.3517 | 20.9061 | 20.4067 | 20.2336 | 20.0427 | 20.2462 | 19.1596 | 18.572 | 18.3832 | 18.5425 | 17.8563 | 17.6859 | 17.1132 | 17.7736 | 17.2601 | 17.1185 | 17.1269 | 16.2023 | 16.7911 | 15.9517 | 15.3654 | 15.2285 | 15.0629

## Slide 12: Different Cathode Material
Cross section of a sample holder with sample being sputtered by Cs+ beam.
From J.S. Vogel
NIM B 361(2015) 156-162
Insert Material | Electron Affinity (eV) | Ion Source Efficiency
Zinc | - | 19.60%
Titanium | 0.085 | 20.60%
Iron | 0.153 | 16.60%
Aluminum (Al2) | 0.433 (1.461) | 11.80%
Molybdenum | 0.747 | 10.30%
Nickel | 1.157 | 5.00%
Copper | 1.236 | 5.50%

## Slide 13: LASER Assisted Sputtering
From Vogel and Giacomo
Radiocarbon V59 (2017) 957-965
10-15% Increase in negative ion current
450 nm 5 W LASER
From Vogel
NIMB V438 (2019) 89-95

## Slide 14: LASER Assisted Sputtering
No increase in
negative ion current
450 nm 5 W LASER
LASER

## Slide 15: LASER Assisted Sputtering
2-3% Increase in negative ion current
450 nm 5 W LASER

## Slide 16: Summary
The development of AMS was/is intimately linked to negative ion cesium sputter sources.
The development of negative ion cesium sputter sources was/is intimately linked to the development of AMS.
Despite decades of development, the ion source remains the most maintenance-intensive and least-understood component of an AMS system.

## Slide 17: Thank you