## Slide 1
E×B Plasma Generated by Electron Beams and Non-thermal Electrons for Materials Processing
Yevgeny Raitses
Princeton Plasma Physics Laboratory, Princeton, NJ, USA
NIBS’ 2026
Nelson, September 2026

## Slide 2
Experiment Team1: Nirbhav Chopra, Stas Musikhin, Ivan Romadanov, Yerbolat Ussenov, Eduardo Rodrigues, Sunghyun Son
Collaborators:
Plasma modeling: Andrei Smolyakov2 and Mikhail Tyushev2
2D Materials: Saien Xie,3 Shoaib Khaild,1 and Igor Kaganovich1
Diamond: Kai-Mei Fu,4 Christian Pederson,4 and Alastair Stacey1
1
2
4
3

## Slide 3
Outline
Motivation: 2D materials for microelectronics
Plasma-enabled 2D materials
    e-beam E×B plasma (Penning source) for gentle processing
        Ion energy, dose of plasma exposure, plasma stability
Next: DEA and negative ions for processing

## Slide 4
Motivation: from microelectronics to nanoscale electronics
G.-H. Lee et al., ACS Nano (2015)

## Slide 5
Background: 2D Transition-metal dichalcogenides (TMDs)
High Mobility at Nanoscale
Nature 499, 419 (2013)
2D TMDs: MX2
Stable van der Waals surfaces
Direct bandgap, 1.5-2.2 eV
Tunable properties
Heterostructures
Y. Liu et al., Nature 591 (2021)

## Slide 6
Plasma processing of MOCVD growth 2D TMDs
Examples of 2D MoS2 processing in inert gas RF plasmas
H. Suzuki et al., Nano Lett. 23 (2023)
MOCVD growth of 2D MoS2 film
Exposure to ICP plasma

## Slide 7
Measures recombination of electrons and holes in TMD
Sensitive to changes in the electronic structure
Sensitive to defects, doping, and strain
Valence Band
Conduction Band
X0
XD
Eg
Eb
e-
e-
h+
Plasma effects on optical properties of TMDs
Ex-situ photoluminescence (PL) spectra of monolayer WS2, before and after argon plasma exposure
~1.67 eV
X0 peak
XD peak
From DFT, XD~ 1.62 eV corresponds to sulfur vacancy defect
Notes: Missing sulfur atoms(S vacancy) create defect sites in MoS₂
These defect sites can trap excited electrons
Trapped electrons can emit light at a lower energy, around 1.62 eV

## Slide 8
Sputtering of TMD by argon ions
Sputtering studies using ab-initio Molecular Dynamics for various Ar ion energies
Sputtering energy threshold for sulfur from MoS2, 30 eV
Y. Polyachenko et al., J. Phys. Chem. Lett. 17 (2026)

## Slide 9
RF ICP: Plasma measurements (EEDF, OES, IEDF)
13.56 MHz, RF ICP reactor
Operating regime
Power: 80 W
Gas: Argon
Pressure: 10 mtorr
Coupling | Te, eV | Ne, cm-3
Reduced C. | 2.6 | 0.5 x 1010
C coupling | 3.6 | 1x 1010
Sheath-presheath voltage drop
Expected ion energies for Ar ions:
  30 eV

## Slide 10
ICP-induced damage to 2D materials
Operating regime
Power: 80 W
Gas: Argon
Pressure: 10 mtorr
Reduced C-mode
Ion energies with RPA
Ex-situ Photoluminescence (PL) at 23 cm
Ion energies:
  30 eV

## Slide 11
Plausible explanation of low ion energy damage to TMD
In oxidized MoS₂, sulfur sputtering by Ar ions is via formation and desorption of stable SO₂, whereas in pristine MoS₂ it is driven by mechanical bond breaking and Sₙ cluster formation.
Because of a stronger electronegativity, Oxygen-Sulfur bound weakens Sulfur-Moly bonds.
Oxygen in the ICP reactor could be from a water residual: base pressure ~ 10-4- 10-5 Pa.
Similar reduced sputtering yield is predicted for fluorinated MoS2 with formation SF4.
If TMD is oxidized, sputtering energy threshold of sulfur, drops 2.5 times (from ab-initio MD)
For oxidized MoS2, sputtering of sulfur by Ar ions 12 eV
Y. Polyachenko et al., J. Phys. Chem. Lett. 17 (2026)
To avoid sulfur sputtering electron temperature should be  2.5 eV

## Slide 12
Access to lower ion energies with E×B Penning source
12
Applied voltage to extract and energize electrons from the cathode and generate the plasma
Applied B-field to reduce the spread of electrons by collisions with neutral atoms, and to separate regions with energetic plasma (center) and cold plasma (vicinity)
  Magnetized electrons and weakly magnetized ions
Cathode diameter ~ 1 cm, is much smaller than the E×B region, ~ 10 cm
2 keV x 1 mA e- beam in Argon gas
100 mtorr, B= 100 Gauss
or Floating boundary (conductive or dielectric)
10 cm
Notes: 12

## Slide 13: Studied cases of plasma boundaries
In a stead-state, the ionization, , is balanced by electron and ion fluxes to the cathode, anticathode and by cross-field transport the chamber wall (anode).
Chopra, Romadanov, YR, Plasma Sources Sci. Technol. 33 (2024)
Tyushev, Papahn Zadeh, Sharma, Sengupta,YR, Boeuf, Smolyakov, Phys. Plasmas 30 (2022)
Floating (metal or dielectric)
13

## Slide 14
Research resources, http://pcrf.pppl.gov
PPPL E×B LTP setups accessible to major plasma diagnostics
Andrei Smolyakov’s group at University of Saskatchewan using 2D & 3D WarpX, 2D EDIPIC, and 3D Vsim by Tech-X
All diagnostics are available through PCRF!
20cm
Up to 100cm
Advanced kinetic simulations:
Snapshot of simulated ion density
14
Notes: 14

## Slide 15: Radial (B) profiles of EEDF, plasma density & electron temperature
Time-averaged plasma properties measured by probes in e-beam E×B plasma at 0.2 mtorr Argon
Chopra et al., Plasma Sources Sci. Technol. 33 (2024)
15
EEDF
Plasma density, cm-3
Electron temperature, eV
Langmuir
Probe

## Slide 16: Radial (B) profiles of plasma potential with emissive probe
Chopra et al., Plasma Sources Sci. Technol. 33 (2024)
Chopra et al., Appl. Phys. Lett. 124 (2024)
16
From emissive probe, ion trapping configuration with E-field directed inward
From LIF, at the axis – small pressure gradient directed inward
Expect no outward-directed ion flow to the substrate

## Slide 17: Time-average Laser-Induced Fluorescence: back ion flow
Ion temperature
Ion velocity and directed against local E-field
Higher ion energies away from the e-beam
Ion energies ~ 0.1 eV, i.e. much less than the threshold for sulfur sputtering ≥ 10 eV
17
Son et al., Plasma Sources Sci. Technol 34 (2025)
Most probable ion velocity
Outward flow
Axis

## Slide 18
Ion heating by plasma instabilities
Azimuthal oscillations (~ 10 kHz), often m=1, much slower than frequency
Ions heated up at plasma periphery
ExB spoke, 104 Hz
Ion heating by spoke, EDIPIC-2D
18
M. Tyushev et al., Phys. Plasmas 30 (2023)
M. Papahn Zadeh et al., Plasma Sources Sci. Technol. 34 (2025)
PIC simulations predict that peak ion energies during oscillations can be sufficient to damage the substrate!
Notes: 18

## Slide 19
Exposure of WS2 to e-beam E×B plasma: Photoluminescence at RT
19
X0
XD
longer exposure
Wavelength / nm
Changes in PL signal (possible damage to TMD) increase with the exposure time.
Measured time-average ion energies are small < 0.5 eV, but in fluctuations ion energies are ~ 15eV, sufficient to knock out sulfur from TMD.
Notes: 19

## Slide 20
Gradient drift instability: collisionless Simon-Hoh instability1
Equilibrium
Density perturbation
Perturbation
Sakawa at al., Phys. Fluids B: Plasma Phys. 5 (1993)
Smolyakov et al., Plasma Phys. Control. Fusion 59 (2017)
  Conditions: neo  0 and neo  Er0 > 0
Wci << w << Wce
20
Notes: 20

## Slide 21
Gradient drift instability: modified Simon-Hoh instability (MSHI)1
1Smolyakov et al., Plasma Phys. Control. Fusion 59 (2017)
2Rodriguez et al. Phys. Plasmas 26 (2019)
21
- ion response
-electron diamagnetic drift frequency
- E×B drift frequency
- ion sound speed
For simplicity, assuming no ion flow: the MSHI instability growth rate2
Dispersion relation of MSHI1
Notes: 21

## Slide 22: Suppression of spoke oscillations with electron collecting boundary
Oscillations of the plasma density (probe measurements) with different boundaries
22
1Rodriguez et al., Phys. Plasmas 26 (2019)
2Chopra and YR, Appl. Phys. Lett. 126 (2025)

## Slide 23
Photoluminescence signal after exposure to a quiet plasma

## Slide 24
Concluding remarks
24
Plasma-induced damage of 2D WS2 observed for ion energies much lower than sputtering yield of sulfur atoms (10x).
Plausible mechanisms are related to:
  plasma-chemical reactions such as oxidation by residual impurities (e.g. water)
  defects in MOCVD produced TMDs
  plasma oscillations and associated oscillations of the ion energy
Minimizing damage
  by minimizing the dose of plasma exposure and impurities in the reactor
  by mitigating oscillations
Next: controlled removal of sulfur utilizing halogenated surfaces exposed to cold plasma, and dissoative electron attachment (i.e. formation of negative halide ion).
Notes: 24

## Slide 25
Acknowledgement
Research is based upon work supported by the U.S. Department of Energy, Office of Science, Fusion Energy Sciences and Basic Energy Sciences, as part of the Extreme Lithography & Materials Innovation Center (ELMIC), a Microelectronics Science Research Center (MSRC) through the Plasma-enabled 2D Materials project at the Princeton Plasma Physics Laboratory (PPPL), under contract number No.DEAC02-09CH11466.
http://elmic.ppp.gov
25
Notes: 25

## Slide 26
MSRC project: Plasma-enabled 2D Materials (PlasMat2D)
6 institutions
19 researchers
Yerbolat Ussenov
Igor
Kaganovich
Thrust 2 Lead
Barry Rand
Co-Director
Alice Kunin
Vincent
Donnelly
David Graves
Thrust 3 Lead
Mark Kushner
Jane Chang
Saien Xie
Thrust 1 Lead
Yevgeny Raitses
Director
Jeremy Mettler
Yury Polyachenko
Seamus Lowe
Connor Reilly
Russell Kwon
Goncalo Cardoso
Shoaib Khalid
Sei-won Chung
Daniel Cho
Satya Butler
Jingtao Tan
Stanislav Musikhin
Eric Joseph
Industry AC
Robert Bruce
Luxherta Buzi
Xavier
Lee
Sofiia Yarytska
Justin
Boles
11 students
Marco
Hopstaken
Lynne Gignac

## Slide 27
Princeton Collaborative Low Temperature Plasma Research Facility (PCRF)
Experts in plasma theory, modeling, experiments and diagnostics
Advanced diagnostics of plasma, flow, nanoparticles, plasma-surface interactions (charging, emission)
Wide range of plasma sources for basic LTP science and applied plasma research
Mist-plasma jets
Low pressure ExB plasma
Scalable flexible DBDs
Arc discharges
e-beam generated LTPs: low to moderate (~ torr) pressures
ExB Plasma thruster physics
1-D, 2-D and 3-D PIC, hybrid, fluid codes
3-D PIC: ExB plasma structures
CFD, nano, diamond for QIS
Basic LTP science
Advanced atomic scale materials processing for microelectronics
Plasma for sustainability
Decarbonization and dusty plasmas
Plasma for healthcare, energy environmental, catalysis applications
Unique computational resources: codes, HPC: CPU-GPU hybrid architecture with open codes
Notes: 27

## Slide 28
http://pcrf.pppl.gov

## Slide 29
Additional remarks
29
CVD grown WS2
For cracks, voids and edges in TMD, AIMD predicts the reduced energy threshold for sulfur sputtering ~ 4eV
Changes of PL when exposed to ambient atmosphere, even without plasma – indicative of chemically driven modifications + light
With plasma, degradation processes may be accelerated.
Kept in ambient
Notes: 29